Phase Field Solidification Modeling
Sam Britt
December 14, 2012

---
Solidification
- Casting, welding
- Consider:
  - Nucleation and growth (hetero/homogeneous)
  - Thermal and constitutional undercooling
  - Solute segregation
  - Cellular and dendritic growth
  - Multi-phase systems, decomposition

---
Solidification Microstructures
Eutectic in cast Cu
George Langford, MIT
Classic Casting
microstructures
Kelton and Greer (2010)
Serious impact on
mechanical properties!
Dendrites in Ni-based superalloy weld
David et al. (2003)

---
Modeling Solidification
- Option 1: “Sharp Interface Model”
  - Explicitly keep track of the interface
  - Conserve heat, mass in solid & liquid, couple with transport eqns. across boundary, add interfacial effects
  - Very computationally intensive for complex, realistic microstructures

---
Modeling Solidification
- Option 2: “Phase Field” (diffuse interface) model
  - Order parameter φ: a field that describes the phase:
    - Where φ = 1, solid. Where φ = 0, liquid.
    - Where 0 < φ < 1, “Interface”
  - Interface is not tracked, but φ is allowed to evolve

---
Governing Equations
“Gradient energy coefficient”
Only non-zero at interface
Contributions from pure phases
“Interface mobility”
(for non-isothermal case)
(interpolation)
(double well)

---
Anisotropy
To model, e.g., dendrites, need anisotropic (direction-dependent) crystal growth: use gradient energy coefficient
2D phase field simulation of dendrites (not mine)
Furrer (2011)

---
This Work
- Implemented single component 1-D phase field simulator for solidification
  - With clear hooks to extend to 2-D and binary systems
- Numerically integrated governing equations using implicit finite difference scheme
  - Explicit scheme required extremely small timesteps
  - Converted finite difference equations to matrix form, solve with LAPACK

---
1D Solidification of ~Ni
ε = 1
M = 1
φ
t
ε = 2
M = 0.5
ε = 1
ε = 1
M = 0.5
M = 0.5
x